## Slide 1: Evolution of Single Atom Pt Sites during Non-oxidative Coupling of Methane
Scientific Achievement
Microscopy and spectroscopy were used to understand the nature of Pt single atom active sites during non-oxidative coupling of methane (NOCM).
Research Details
  Single atom Pt on CeO2 and Pt nanoparticles (~2nm) on SiO2 show similar ethylene formation rates.
  Pt found to sinter to particles approximately 5–7 nm in size, suggesting that single atoms do not survive industrial NOCM reaction conditions.
  Study suggests Pt single atoms are not the active sites for NOCM.
Significance and Impact
NOCM converts methane to higher hydrocarbons and elucidating the mechanism and is critical for the development of shale gas and tight oil reserves.
Talpade, A. D.; Canning, G.; Zhuchen, J.; Arvay, J.; Watt, J.; Miller, J. T.; Datye, A.; Ribeiro, F. H. Catalytic Reactivity of PT Sites for Non-Oxidative Coupling of Methane (NOCM). Chemical Engineering Journal 2024, 481, 148675.
HR-TEM images of spent a) 2 wt% Pt/SiO2 and b) 1 wt% Pt/CeO2 catalyst, and NOCM Kinetic studies.
Notes: 1-2 paragraph description of highlight – The development of shale gas and oil reserves could lead to an increase in natural gas production of 100% by 2050, and methane can account for 70-90% of the shale gas source. Therefore, conversion of methane to higher order organics is a critical technology. Recently, single atom catalysts have been suggested as stable and non-coking catalysts for non-oxidative coupling of methane (NOCM) to ethylene and higher hydrocarbons. It is speculated that the active site catalyzes the CH abstraction of methane to give methyl radicals. These radicals combine in the gas-phase to yield a hydrocarbon product distribution comprising of ethylene, propylene, benzene, and naphthalene. However, the exact nature of the active site under reaction conditions remains yet to be understood. In this work, the aim was to investigate the kinetics of non-oxidative coupling on single site Pt/CeO2 catalysts and compare them to the performance on Pt nanoparticles (Pt/SiO2) and with the empty reactor, which serves as a surrogate for gas phase kinetics.
However, on the Pt single atom sites on ceria, we did not detect any improvement over Pt nanoparticle catalysts as claimed in the literature. This was shown by the similar kinetic performance of the Pt SA and NP catalysts indicated by the similar ethylene formation rates. The Pt sites are found to sinter and coke, evidenced through TEM studies indicating clustering of Pt to 5–7 nm in the materials following NOCM. Ethylene hydrogenation experiments and CO-IR spectroscopy confirm the sintering and loss of isolated surface Pt species under reaction conditions. In conclusion, these studies indicate that the single Pt atoms are not the active sites for NOCM.
Acknowledgements – This work was supported by the National Science Foundation under Cooperative Agreement No. EEC-1647722. The TEM work was performed at the Center for Integrated Nanotechnologies, an Office of Science User Facility operated for the U.S. Department of Energy (DOE) Office of Science by Los Alamos National Laboratory (Contract 89233218CNA000001) and Sandia National Laboratories (Contract DE-NA-0003525).
Publication/ press releases/ related links:
Talpade, A. D.; Canning, G.; Zhuchen, J.; Arvay, J.; Watt, J.; Miller, J. T.; Datye, A.; Ribeiro, F. H. Catalytic Reactivity of PT Sites for Non-Oxidative Coupling of Methane (NOCM). Chemical Engineering Journal 2024, 481, 148675. DOI:10.1016/j.cej.2024.148675.