## Slide 1: Large-Scale Optical Characterization of Solid-State Quantum Emitters
Scientific Achievement
Parallel characterization of photoluminescence excitation (PLE) from diamond-based color centers leading to a >100 X speed-up in characterization time.
Research Details
  Diamond is fabricated with QR-code like features encoding location information.
  The diamond is then implanted with 29Si using a Wien filter focused ion beam system.
  Color centers formed after annealing are uniquely identifiable by their adjacent QR code.
  A widefield PLE setup is used to characterize color centers in parallel.
Significance and Impact
Solid-state color centers are an emergent quantum memory platform with diamond-based color centers attracting significant interest due to the possibility of having a nuclear spin free bath in isotopically purified 12C. Currently, color centers in diamond are characterized serially through confocal microscopy. This work registers color centers to machine-readable coordinates enabling automatic, parallel characterization.
This work was performed in part at The Center for Integrated Nanotechnologies.
Yuan, R.; Kumar, A.; Zhuang, S.; Cucciniello, N.; Lu, T.; Xue, D.; Penn, A.; Mazza, A. R.; Jia, Q.; Liu, Y.; Xue, D.; Li, J.; Hu, J.-M.; LeBeau, J. M.; Chen, A. Machine Learning-Enabled Superior Energy Storage in Ferroelectric Films with a Slush-like Polar State. Nano Letters 2023, 23 (11), 4807–4814. DOI:10.1021/acs.nanolett.3c00277.
Widefield fluorescence image of FIB implanted SiVs reconstructed from PLE scans.
Histogram showing inhomogeneous distribution of SiV PLE from 40186 peaks with linewidth < 2GHz.
Whitelight image of QR code with adjacent implant region
(a) Design of QR codes (i) Alignment markers (ii) Human readable position information (iii) Machine readable position information (b) Post-processed QR data spanning the QR encoded coordinate system
a
b