## Slide 1: Influence of Alloy Interfacial Layers in Anode-Free Solid-State Batteries
Scientific Achievement
This study provides new insights into the mechanisms through which alloy (Au and Ag) interfacial layers influence lithium deposition/stripping, revealing methods to improve the performance of anode-free solid-state batteries.
Research Details
  100-nm Ag or Au films were evaporated onto the Cu current collector before cell assembly.
  Alloy interlayers enable stable cycling and improved Coulombic efficiency.
  FIB-SEM and X-ray computed tomography reveal lithium morphology.
  Impedance spectroscopy shows that alloys mitigate contact loss during stripping.
  Interfacial engineering may be necessary to enable anode-free solid-state batteries
Significance and Impact
‘‘Anode-free’’ solid-state batteries exhibit improved safety and high energy density due to the lack of active material at the anode. To enable this technology, it is necessary to spatially control the evolution of lithium during charging. This work focuses on the influence of alloy interfacial layers on lithium cycling during battery operation, and it shows that alloy layers favorably control anode morphology for improved battery performance.
Sandoval, S. E.; Lewis, J. A.; Vishnugopi, B. S.; Nelson, D. L.; Schneider, M. M.; Cortes, F. J.; Matthews, C. M.; Watt, J.; Tian, M.; Shevchenko, P.; Mukherjee, P. P.; McDowell, M. T. Structural and Electrochemical Evolution of Alloy Interfacial Layers in Anode-Free Solid-State Batteries. Joule 2023, 7 (9), 2054–2073.
Li grows much more uniformly on the alloy-coated electrodes with thicknesses closer to the expected theoretical value for both (5.3 and
5.1 mm at the thickest points for Ag- and Au-coated electrodes, respectively). The alloy-modified cells also do not exhibit obvious Li growth within the solid-state electrolyte (SSE) pores, which likely arises from the more uniform nucleation enabled by the alloys.
This work was performed in part at The Center for Integrated Nanotechnologies.
Notes: 1-2 paragraph description of highlight –
While there has been a large body of work focused on understanding Li deposition/stripping behavior in Li-excess metal batteries using both solid and liquid electrolytes, there has been minimal focus on understanding Li behavior in anode free solid-state batteries (SSBs). Interfacial materials, including Li alloys and others, have previously been investigated in anode-free and Li-excess SSBs to improve cycling. Silver (Ag)-carbon composite layers can facilitate uniform cyclic Li deposition/stripping. Telluride layers have also been shown to promote uniform growth. Li-magnesium alloy interfaces can enhance diffusion and diminish voiding. While these studies have shown improved cell performance, there is a lack of knowledge of the mechanistic influence of interfacial layers on the evolution of Li in anode-free SSBs.
Here, CINT Users and CINT Scientists investigate the structural and electrochemical evolution of Ag and gold (Au) alloy interlayers in sulfide (Li6PS5Cl [LPSC]) anode-free SSBs, finding that these materials enable uniform Li growth/stripping and act to mitigate contact loss at the end of stripping through responsive current homogenization. Both alloy layers enhance cycling stability and CE compared with bare copper (Cu).
Acknowledgments –
This work was supported by the Center for Mechano-Chemical Understanding of
Solid Ion Conductors (MUSIC), an Energy Frontier Research Center funded by the
US Department of Energy (DOE), Office of Science, Office of Basic Energy Sciences
under contract DE-SC0023438. A portion of this work was performed at
the Center for Integrated Nanotechnologies, an Office of Science User Facility
operated for the US DOE, Office of Science. Los Alamos National Laboratory,
an affirmative action equal opportunity employer, is managed by Triad National
Security, LLC for the US DOE’s NNSA, under contract 89233218CNA000001. This
research additionally used resources of the Advanced Photon Source, a US DOE
Office of Science User Facility operated for the DOE Office of Science by Argonne
National Laboratory under contract no. DE-AC02-06CH11357. S.E.S acknowledges
support from an NSF Graduate Research Fellowship under grant
no. DGE-1650044, US DOE Office of Science Graduate Student Research
(SCGSR) program under contract no. DE-SC0014664, and a Sloan Foundation
MPHD Program Scholarship.
Publication/ press releases/ related links:
https://www.sciencedirect.com/science/article/pii/S2542435123003203