## Slide 1: Patterned Electron Probes Enable Direct Measurement of the Thermal Expansion Coefficient of an Atomically Thin Semiconductor
Scientific Achievement
Discovery that patterned electron probes yield an extra level of precision in measuring lattice parameters enabling direct measurement of the thermal expansion coefficient (TEC) of a 2D material, WSe2, which is promising as it falls within the value of conventional materials used in microelectronics.
Research Details
  Heating experiments were performed on wafer-scale polycrystalline monolayer WSe2 transferred onto TEM grids with 2 mm diameter holes, and heated in a furnace-style sample holder.
  4D-STEM was performed at 60 keV from room temperature up to ~550 °C, and detailed computational processing performed to obtain the evolution in lattice parameter statistics as the sample was heated. This was compared against density functional theory calculations.
Significance and Impact
Our discovery establishes that the in-plane TEC of large-scale polycrystalline monolayer WSe2 [(3.5±0.9)×10-6 K-1] is indeed more in line with the bulk TEC, while the out-of-plane TEC [(57±20)×10-6 K-1] is an order of magnitude larger than bulk.
Kucinski, T.;Dhall, R.; Savitzky, B.; Ophus, C.; Karkee, R.; Mishra, A.; E. Dervishi, E.; Kang, J.H.; Lee, C.-H.; Yoo, J.; Pettes, M.T. "Direct Measurement of the Thermal Expansion Coefficient of Epitaxial Wse2 by Four-Dimensional Scanning Transmission Electron Microscopy," ACS Nano 2024, 18, 17725–17734, DOI: 10.1021/acsnano.4c02996.
(left) Exaggerated depiction of scattering from the complex-shaped electron probe and (right) experimental changes in lattice parameters with temperature used to obtain the TEC of 2D WSe2.
Work was performed, in part, at the Center for Integrated Nanotechnologies.
Notes: 1-2 paragraph description of highlight – NOT the abstract of the paper… more like talking points for a non-expert speaker using the slide that summarize the most important aspects .
Future microelectronic technology will require integration of advanced materials such as two-dimensional (2D) semiconductors for improved performance, however, operation of such devices generates heat which can impact their function including delamination and device failure. Heating a material usually results in the atoms arranged within the lattice to expand but things “get weird” when materials become only one to a few atoms thick. At such extremes, these 2D materials behave differently including the degree of thermal expansion and even the possibility of contraction, and existing experimental techniques have drawbacks that have led to large discrepancies of reported values in the literature.
In new collaborative work between the Center for Integrated Nanotechnologies, The Molecular Foundry, and Seoul National University, a new methodology for measuring precise lattice parameters is presented which employs a complex-shaped electron beam and four-dimensional scanning transmission electron microscopy (4D-STEM) and computational analysis of these datasets to reveal the local material structure as a function of temperature for accurate determination of thermal expansion.
We are the first to show that nanometer scale electron diffraction can be used to measure strain and orientation sensitively enough to measure a weak thermal effect, demonstrated in our paper by measuring thermal expansion in the two-dimensional semiconductor tungsten diselenide. Before this the scientific community thought this could not be done with TEM since the rule of thumb is that quantitative electron diffraction has about a 2 % uncertainty, but thermal expansion would require uncertainty better than 0.01 %. Patterned electron probes, first invented by The Molecular Foundry, allowed us to reach this low uncertainty level.
Acknowledgements – from the paper, with additional info if the acknowledgement is not sufficient to list the organizations that supported the research.
This work was supported by the Laboratory Directed Research and Development program of Los Alamos National Laboratory under project numbers 20230014DR, 20220485MFR, 20190516ECR, and National Security Education Center under project numbers IMS RR19PETT, IMS RR21PETT, and ISTI IP2104MP. Work at the Molecular Foundry was supported by the Office of Science, Office of Basic Energy Sciences, of the U.S. Department of Energy under Contract no. DE-AC02-05CH11231. C.O. acknowledges additional support from the Department of Energy Early Career Research Award program. C.-H.L acknowledges the support by the National R&D Program through the National Research Foundation of Korea (NRF) funded by the Ministry of Science and ICT (2023R1A2C3005923 and 2020M3D1A1110548). This work was performed in part at the Center for Integrated Nanotechnologies, an Office of Science User Facility operated for the U.S. Department of Energy (DOE) Office of Science. Los Alamos National Laboratory, an affirmative action equal opportunity employer, is managed by Triad National Security, LLC for the U.S. Department of Energy's NNSA, under contract 89233218CNA000001.
Publication/ press releases/ related links:
https://discover.lanl.gov/news/0627-atomically-thin-materials/