## Slide 1: Solution-Processed Ultrafast, Room-Temperature Single-Photon Source at 1550 nm
Scientific Achievement
Created fastest (12.6 MHz) C-band room-temperature deterministic single-photon source (SPS) by integrating PbS/CdS quantum dot (QD) and plasmonic nanogap antenna
Research Details
  Fabricated ensemble and single cavity-coupled QDs.
  Studied effects of excitation and emission enhancement on photoluminescence (PL) revealing extreme Purcell enhancement factors to 10,700 and ultrafast PL lifetimes (to 65 ps).
Significance and Impact
Addressed key limitations of telecom SPSs toward new quantum technologies: instability, need for cryogenic operation, or long radiative lifetimes that limit brightness and speed.
(a) Solution-processed room-T C-band SPS. (b) PL spectrum of a single cavity-coupled QD. (c) Fast PL decay only in cavity. (d) 1550 nm SPS power-dependent counts-per-second (cps) (uncorrected)
PL (norm.)
PL (norm.)
Time (ns)
Wavelength (nm)
PL (cps)
Power (W/cm2)
a
b
c
d
This work was performed, in part, at The Center for Integrated Nanotechnologies.
Zhang, S.; Traverso, A. J.; Dolgopolova, E. A.; Singh, A.; Kishida, H.; Livshits, M. Y.; Sheehan, C. J.; Bowes, E. G.; Li, C.; Hollingsworth, J. A.; Mikkelsen, M. H. Solution-Processed Ultrafast, Room-Temperature Single-Photon Source at 1550 Nm. ACS Nano 2025.
Notes: 1-2 paragraph description of highlight –
*Demonstrated an ultrabright, room-temperature, single-photon source based on colloidal QDs capable of emission in either the O- or C- telecom bands.
*The traditional drawbacks of the employed colloidal emitters, including long emission lifetime, low quantum yield, and nondirectional emission, have been addressed by the nanocavity, yielding high brightness, short emission lifetimes, and stable, nonblinking emission.
*These cavity-coupled QDs comprise the brightest single photon source at room temperature demonstrated to date and one of the brightest single-photon sources demonstrated at telecom C-band.
*Verifies the single-photon action of the nanocavity-coupled QDs by showing room-temperature antibunching dip.
*Alternative material platforms for single photon sources (SPSs), such as epitaxially grown QDs, carbon nanotubes, and defects in two-dimensional transition metal dichalcogenides, have shown narrower line widths from a few meV to sub-meV and high photon purity with g(2)(0) < 10–2 in the telecom band. However, these platforms are challenged by difficulties in room-temperature operation, scalability, and consistency in wavelength.
*Nanocavity-coupled colloidal QDs present a promising pathway toward achieving a highly tunable and scalable single-photon source at room temperature.
*With the nonblinking characteristic, the nanocavity-coupled QDs are close-to-ideal candidates for quantum communication applications.
*Colloidal QDs have found widespread use in classical optoelectronics, from television screens to color-changing LED lights, and their established device integration may help propel their future impact in quantum information technologies.
Acknowledgements – FundingM.H.M. acknowledges support from the Air Force Office of Scientific Research (award FA9550-21-1-0312) and the Gordon and Betty Moore Foundation through Grant GBMF8804. M.H.M. and J.A.H. acknowledge partial support from the U.S. Department of Energy, Office of Science, Office of Basic Energy Sciences under Triad National Security, LLC contract grant 89233218CNA000001 [FWP: LANLE1N3]. This work was performed in part using instrumentation at the Duke University Shared Materials Instrumentation Facility (SMIF). SMIF is a member of the North Carolina Research Triangle Nanotechnology Network (RTNN), which is supported by the National Science Foundation (Grant ECCS-1542015), as part of the National Nanotechnology Coordinated Infrastructure (NNCI). This work was conducted in part at the Center for Integrated Nanotechnologies (CINT), a Nanoscale Science Research Center and User Facility operated for the U.S. Department of Energy (DOE), Office of Science (SC), Office of Basic Energy Sciences (BES) (User Project: 2022AC0150). E.A.D. and A.S. were supported by Los Alamos National Laboratory (LANL) Director’s Postdoctoral Fellowships (20190620PRD1, 20160653PRD2). M.Y.L. acknowledges the LANL Seaborg Institute for a postdoctoral fellowship. C.J.S. and E.G.B. were funded by CINT. J.A.H. was supported by the LANL Laboratory Directed Research & Development program (20230363ER). LANL is operated by Triad National Security, LLC, for the National Nuclear Security Administration of U.S. Department of Energy (Contract no. 89233218CNA000001).
Publication/ press releases/ related links: TBD
ACS Nano 2025: https://doi.org/10.1021/acsnano.4c18261